Refractive Indices and Infrared Band Strengths of Amorphous Ices of Key Fluorinated Refrigerants 1,1,1,2-Tetrafluoroethane, 2,3,3,3-Tetrafluoropropene and 3,3,3-Trifluoropropene

Koushik Mondala, Mason McAnallya, Souvick Biswasa, Nils Melbournea, Andrew M Turnera, Alexandre Bergantinia,b, Rui Suna*, Ralf I. Kaisera*

a Department of Chemistry, University of Hawai’i at Manoa, Honolulu, Hawaii 96822, United States

bPresent Address: Valongo Observatory, Federal University of Rio de Janeiro (OV-UFRJ), Rio de Janeiro-RJ, 20080-090, Brazil

* Corresponding author. E-mail: ruisun@hawaii.edu; ralfk@hawaii.edu

Keywords: refrigerant, low temperature, solid, infrared spectroscopy, interferometry

Abstract

Hydrofluorocarbons (HFCs), a class of polyfluorocarbon (PFC), represent a key group of chemicals exploited extensively in refrigeration and innovative future technological cooling applications. To separate, purify, and reuse HFCs, spectroscopic properties of these compounds must be available. To quantify these materials under cryogenic conditions, a condensed phase spectroscopic investigation of their physical parameters is required. This study investigates the optical and spectroscopic properties of hydrofluorocarbons used as refrigerant at low-temperature (10 K). Refractive indices of 1,1,1,2-tetrafluoroethane (CF3CH2F; HFC134a), 2,3,3,3–tetrafluoropropene (CF3CF=CH2; R1234yf), and 3,3,3–trifluoropropene (CF3CH=CH2; R1243zf) are found to be 1.24 ± 0.02, 1.34 ± 0.02, and 1.30 ± 0.02, respectively. Infrared band strengths of the abovementioned HFC ices on a cold silver substrate were measured utilizing absorption reflection infrared spectroscopy. The fundamental vibrational modes were analyzed using quantum chemical calculations in tandem with vibrational spectroscopic analysis. The strongest infrared absorption corresponds to combined C—F vibrational modes originating from CF3 group and olefinic C—F bonds, which has band strengths ranging 2×10-18 to 3×10-18 cm molecule-1. Comparisons of solid and vapor phase spectra show vibrational shifts, aiding understanding of solid-state interactions and ice formation. These findings enhance knowledge of low-temperature HFC chemistry, focusing on optical and spectroscopic changes during ice development.

1.Introduction

Perfluorocarbons (PFCs) are a class of chemical compounds distinguished by their exceptional stability, non-flammability, low surface tension, and minimal solubility. These properties render them highly valuable across a broad array of applications, ranging from household products to industrial processes. Notably, a significant subset of fluorinated gases, particularly hydrofluorocarbons (HFCs), are extensively produced and utilized in refrigeration and air conditioning systems.[1-3] Moreover, HFCs are being explored for innovative technological applications, including liquid thin film technologies in aviation and aerospace sectors, as well as advanced cooling systems employing supersonic jet nozzles.[4-6] Ongoing research aims to develop future cooling technologies tailored for critical sectors, emphasizing efficiency and environmental safety.

Despite their widespread use, the environmental fate of HFCs remains not completely understood from a molecular perspective. Specifically, the mechanisms underlying their photolytic breakdown and oxidation are not fully elucidated particularly in the context of upper tropospheric conditions and low-temperature cloud formation.[7-10] This knowledge gap raises concerns about the potential long-term atmospheric consequences of HFC emissions. Consequently, regulatory measures are in place, and researchers are actively exploring policies that promote the recycling of legacy refrigerants, the adoption of environmentally benign alternatives, and the reduction of unintentional atmospheric emissions.[11-13]

Recycling methods for refrigerants, such as cryogenic separation techniques, membrane-assisted cryogenic separation,[14-16]  and extractive distillation using ionic liquids,[17-19] are considered highly effective. These techniques are especially crucial for managing environmentally hazardous HFCs used in ultra-low temperature refrigeration systems, which operate between 223 K and 123 K.[20] Such systems are vital for pharmaceutical and biological applications, where current alternatives are limited. Implementing these advanced recycling methods can significantly reduce environmental risks associated with the disposal and reuse of refrigerants in sensitive applications. New generation refrigerants like 2,3,3,3-tetrafluoropropene (R-1234yf) are already replacing older compounds such as 1,1,1,2-tetrafluoroethane (HFC-134a) in household and automotive industries,[10, 21-24] but substantial gaps remain in understanding their environmental behavior, especially under tropospheric conditions. Concerns have been raised about the formation of persistent chemicals like trifluoroacetic acid (CF3COOH) during their breakdown, which could have significant impacts on the atmospheric chemistry, particularly in low-temperature environments.[25-27] Recent advancements in optical spectroscopic techniques have facilitated the investigation of these processes at the molecular level, providing insights into their behavior in the upper troposphere.[28, 29]

Progress in utilizing the unique properties of HFCs for technological applications, combined with the development of cryogenic separation techniques and studies of low-temperature interactions, underscores the need for reliable spectroscopic quantification of refrigerants under such conditions.[19, 30-32] Although infrared and Raman spectroscopy have been employed to study refrigerants in gas and liquid phases, comprehensive vibrational assignments related to molecular interactions and the quantification of key optical and spectroscopic parameters, such as refractive index, band strength in solid amorphous ices, remain limited.[33-41] Addressing these gaps is essential for advancing our understanding of refrigerant behavior in cold environments.

This combined experimental and computational study aims to quantify critical optical and spectroscopic parameters, including refractive index and infrared band strength. Fundamental spectroscopic properties were determined by exploiting laser interferometry and absorption reflection Fourier transform infrared spectroscopy (FTIR) from the vapor deposited ices of the refrigerants at low-temperature. Such data which is essential to understand their upper tropospheric chemistry. The first system of interest in this aspect is the most extensively used refrigerant for the last several decades, HFC134a [1,1,1,2-tetrafluoroethane; CF3CH2F; (R-I)]. Additionally, the study investigates newer hydrofluoroolefins (HFOs), such as R-1234yf [2,3,3,3-tetrafluoropropene; CF3CF=CH2; (R-II)] and R-1243zf [3,3,3-trifluoropropene; CF3CH=CH2; (R-III)] which are gaining prominence as environmentally friendlier alternatives (Table 1). Overall, this research opens a new and largely unexplored avenue for understanding the low-temperature quantification of HFCs and the evolution of distinctive spectral features in the solid state, further supporting the development of sustainable cooling technologies that minimize ecological impact.

Table 1: Compilation of molecular structures, formulae, common names, and abbreviations used in this publication.

| Structure |  |  |  |
| --- | --- | --- | --- |
| Molecular formula | CF3CH2F | CF3CFCH2 | CF3CHCH2 |
| IUPAC name | 1,1,1,2–tetrafluoroethane | 2,3,3,3–tetrafluoropropene | 3,3,3–trifluoropropene |
| Common name | HFC134a | R-1234yf | R-1243zf |
| Name used here | R-I | R-II | R-III |

2. Experimental and Computational Methods

A schematic presentation of the experimental arrangement is shown in Figure 1. Briefly the experiments were conducted in an ultrahigh vacuum (UHV) chamber manufactured from low-carbon stainless steel type 304.[42-46] The chamber was evacuated to a base pressure of 5 × 10-11 torr using an oil-free, magnetically levitated turbomolecular pump (Osaka, Pump Model TG1121 MCA) in series with a second turbomolecular pump (Osaka, Pump Model TG420 MCAC) backed by an oil-free scroll pump (Edwards, XDS35i). At the center of the chamber, a silver substrate serves as the target affixed to a cold head (CTI Cryodyne 1020C); this target was cooled to 10  0.5 K by a two-stage closed-cycle helium refrigerator (Cryodyne 9600 compressor). The cold head was connected to a differentially pumped rotatable flange allowing the silver target to rotate freely within the experimental plane. The gas deposition onto the target was done by introducing each gas in separate experiments through a glass capillary array with 10 μm pores controlled by a precision leak valve (Figure 1). Neat refrigerant ices were prepared by depositing 99.9 % 1,1,1,2- tetrafluoroethane (R-I) (Chemours), 2,3,3,3-tetrafluoropropene (R-II) (Chemours), and 3,3,3 trifluoropropene (R-III) (Pfaltz & Bauer) at pressures of some 5 × 10-7 torr. The growth patterns of the ice films were controlled by the deposition time and monitored in situ via laser interferometry (Section 2.1).

Figure 1: Schematic representation of the (a) experimental setup, (b) laser interferometry setup and (c) beam path.

2.1. Laser Interferometry

Laser interferometry is primarily used for determining refractive indices, band strengths, and thicknesses of vapor-deposited ices.[42-48] A helium-neon (HeNe) laser with an output of 632.8 nm (λ) (Melles Griot 25-LHP-213, 0.5 mW) is reflected off the silver substrate during the deposition at an angle specified in Figure 1b. The power of the reflected light was monitored with a calibrated photodiode (Thorlabs SM1PD1A) connected to a picoammeter (Keithley 6485) and recorded versus the time using a LabVIEW script. The interference patterns resulting from the constructive and destructive interference between the portion of the laser that reflects off the ice surface with the portion that transmits through the ice and reflects off the silver substrate (Figure 1b) as the ice layer grows, thus altering the optical path difference and phase. Two lasers were positioned at different angles relative to the perpendicular plane of the silver substrate - Laser 1 at (1.9°±0.1°) (θ1) and Laser 2 at (54.8°±0.1°) (θ2) - through conflat (CF) interfaced quartz windows as shown in Figure 1b. The periods between two fringes in the interference patterns for two lasers (T1 and T2) are utilized to calculate refractive index (ηR) according to equation 1.[42]

ηR2=T22T12sin2θ2-sin2θ1T22T12-1                                                         (1)

The calculated refractive index (ƞR) is further utilized to determine ice thickness (d) via same laser interferometry scheme by determining the fringes (n), where λ is the wavelength of the HeNe laser (632.8 nm). This ice thickness (d) combined with an infrared spectrum is necessary to determine infrared band strengths (section 2.2.).

d=nλ2ƞR2-sin2θ1                                                          (2)

Although different thickness ices can be prepared exploiting laser interferometry, there exists some limitations related to ice thickness depending on refractive index, wavelength of the laser used as well as number of fringes formed during deposition.

2.2. Spectroscopic Measurement

To collect infrared spectra at various thicknesses, amorphous ices of specific thicknesses were deposited by introducing refrigerant vapors onto a cold silver substrate at position 1, followed by rotating the substrate to position 2 to record the FTIR spectra in absorption-reflection mode at a 75° reflection angle with respect to the perpendicular axis of silver substrate (Figure 1c). FTIR spectroscopy in the range of 500 cm-1 to 5000 cm-1 was used to measure the infrared band strength. The Nicolet 6700 FTIR spectrometer (Thermo Scientific), equipped with customized external copper mirror optics, has been operated in absorption-reflection mode at a 75° reflection angle (Figure 1c, θ3). The IR beam was focused on the silver substrate through a 35 mm zinc-selenide (ZnSe) window mounted on a CF flange. The reflected IR beam exits through a similar window, was recollimated, and directed to a liquid nitrogen-cooled Mercury Cadmium Telluride (MCT-B) detector via second-stage transfer optics. Spectra were recorded over 30 minutes with a spectral resolution of 4 cm-1, averaging 3360 scans per spectrum for improved signal-to-noise ratio. The infrared beam refracted within the ice at an angle θ4 which is related to angle of incidence IR beam (θ3) according to Snell’s law as:

θ4=sin-1ηvηRsinθ3                                                  (3)

Using this refraction angle optical pathlength (L), the IR beam passes through a definite thickness (d) of ice can be determined as:

L=2dcosθ4                                                             (4)

Although the major objective of the study is to explore quantitative spectroscopic parameters like band strength, FTIR spectra of the deposited ices were also collected at various temperatures up to their sublimation from the silver substrate to gain additional spectroscopic insights.

Apart from the FTIR measurement of the vapor-deposited ice, gas phase infrared spectra of each of the refrigerants were also recorded to compare the spectral shifts and intensity pattern at different stages. However, in this case, infrared spectra of the gases diluted in nitrogen (1:760) at a total pressure of 760 torr were recorded at a spectral resolution of 1 cm-1 in normal absorption mode.

2.3 Computational Methods

The geometries of the refrigerants were optimized and infrared (IR) frequencies for 1,1,1,2-tetrafluoroethane (R-I), 2,3,3,3-tetrafluoropropene (R-II), and 3,3,3-trifluoropropene (R-III) were calculated with the NWChem program suite using density-functional theory at the B3LYP-D3/def2-TZVP level at 0 K.[49] The hybrid B3LYP functional offers a well-documented balance between accuracy and cost for vibrational spectroscopy of halogenated hydrocarbons, while the D3 dispersion correction is included to recover long-range interactions neglected by B3LYP[50]. The triple-zeta valence plus polarization def2-TZVP basis set provides near-basis-set-limit force constants for first-row and fluorine-substituted systems[51]. After full geometry optimization, analytic second derivatives were used to obtain harmonic vibrational wavenumbers.  Unlike to the usual harmonic frequency uniformly scaling as recommended by the NIST Computational Chemistry Comparison and Benchmark Database (CCCBD) for B3LYP/def2-TZVP experimental frequencies  to compensate for systematic overestimation arising from the harmonic approximation and residual basis-set/functional deficiencies[52], we calculated a calibration factor from the slope of the linear fit between experimentally measured frequencies at 10 K and theoretical frequencies at  0 K (Figures S1(a)-S1(c)). The factor determined to be 0.983±0.001, 1.004±0.001 and 0.981±0.001 for R-I, R-II, and R-III refrigerants respectively.

3. Results and Discussions

3.1 Refractive Indices

The interference patterns of vapor-deposited refrigerant ices at 10 K are illustrated in Figures 2(a), (b) and (c) for R-I, R-II, and R-III, respectively. For each refrigerant, the interference patterns obtained with the progress of deposition from the two lasers placed at distinct angles with respect to the perpendicular axis on silver substrate were distinctly different. The upper trace of each figure represents the interference pattern obtained for the photodiode current from the laser placed at 54.8°±0.1° (θ2) while lower trace represents interference pattern generated by the laser placed at an angle of 1.9°±0.1° (θ1) with respect to the perpendicular axis on silver substrate. It is important to note that these fringes should ideally be perfectly sinusoidal. However, fluctuations arising from laser stability and photodiode response can cause deviations in the resultant photodiode current from ideality. To accurately determine the periods T1 and T2 between consecutive fringes, the experimental data, defined by black traces, are smoothed (red) and fitted (green) using a modified sinusoidal function that accounts for these deviations, ensuring that the time axis aligns accurately. The modified sinusoidal function incorporates a linear decay component alongside the standard sine function, as described by equation 5 which is necessary as reflectivity of the silver substrate decreases with the extent of ice deposition, results in decrease in overall photodiode current.

y=y0+ASinπx-xcω+mx                                                    (5)

where xc represents the phase shift, ω is the period, A is the amplitude, y0 is the initial offset, and m denotes the slope of the linear decay. The average time periods between consecutive fringes, derived from the fitted profiles, are taken as the actual periods Tn(1or2). The phase shift error is considered as the measurement uncertainty in these periods. In Table 2, we summarize the fitted interference periods (Tn(1or2)) and the corresponding refractive indices (ηn) of three refrigerants, calculated using equation 1. Our measured refractive index of a known, well-characterized amorphous methane ice at 10 K is compared with the reported literature value;[53] the fringe patterns are shown in Figure S2. The measured refractive index of the amorphous methane ice of 1.36±0.01 in our experiments closely aligns with the reported value of 1.34±0.04. The experimentally measured refractive indices (ηn) of three refrigerants determined through this analysis at 10 K are: 1.24±0.02, 1.34±0.02 and 1.30±0.02 for R-I, R-II, and R-III, respectively. These refractive indices are crucial toward quantifying the integrated absorption coefficients, discussed later in the paper.[47]

Figure 2: Interference pattern formed simultaneously during deposition at different angles in the two-laser interferometry setup. (a) 1,1,1,2-tetrafluoroethane (R-I); (b) 2,3,3,3–tetrafluoropropene (R-II); (c) 3,3,3-trifluoropropene (R-III).

Table 2: Parameters obtained from the fitted interference profiles and corresponding refractive indices.

| Name | Time period for laser-1 (T1) (s) | Time period for laser-2 (T2) (s) | Refractive index (η) |
| --- | --- | --- | --- |
| methane | 61.7 ± 0.3 | 76.9 ± 0.3 | 1.36 ± 0.02 |
| 1,1,1,2-tetrafluoroethane (R-I) | 81.6 ± 0.4 | 108.2 ± 0.2 | 1.24 ± 0.02 |
| 2,3,3,3-tetrafluoropropene (R-II) | 110.6 ± 0.2 | 139.9 ± 0.4 | 1.34 ± 0.02 |
| 3,3,3-trifluoropropene (R-III) | 80.2 ± 0.3 | 103.7 ± 0.7 | 1.30 ± 0.03 |

Table 3: Number of fringes obtained from the laser interferometry for different thickness of refrigerant ices.

| Name of the compound | Refractive index (η) | Number of fringes (n) | Thickness of ice (d) (nm) |
| --- | --- | --- | --- |
| 1,1,1,2-tetrafluoroethane (R-I) | 1.24±0.02 | 2.0±0.1 | 518±16 |
|  |  | 4.1±0.1 | 1037±21 |
|  |  | 6.1±0.1 | 1556±24 |
| 2,3,3,3-tetrafluoropropene (R-II) | 1.34±0.02 | 2.1±0.1 | 504±15 |
|  |  | 4.3±0.1 | 1015±18 |
|  |  | 6.3±0.1 | 1486±21 |
| 3,3,3-trifluoropropene (R-III) | 1.30±0.03 | 2.0±0.1 | 486±14 |
|  |  | 4.3±0.1 | 1046±20 |
|  |  | 6.2±0.1 | 1508±26 |

3.2 Spectral Assignments and Infrared Band Strengths of Refrigerants in Amorphous Ices

Although the vibrational modes of HFCs are well established in the gas and liquid phases, quantitative information on their absorption coefficients in the solid phase is still insufficient. Previous spectroscopic studies of low-temperature solid HFCs have been mostly performed at 150 K, and quantitative information of the band strengths are lacking. The present, low-temperature, contamination-free, vapor deposition, combined with optical interferometry and highly sensitive absorption-reflection-absorption infrared spectroscopy, has the capability to meticulously monitor spectroscopic properties of thin ice layers down to a few nanometers with high accuracy. Additionally, we discuss spectral changes with varying ice layer thicknesses.

3.2.1 Band Assignments

For each of the refrigerant, infrared spectra corresponding to three different ice thicknesses (d) were recorded (Figures 3-5). The thicknesses of the ices were obtained via the number of fringes collected by laser interferometry similar to refractive index measurements. In case of R-I, the depositions of the refrigerant vapor on cold silver substrate were stopped after forming 2.0±0.1, 4.1±0.1 and 6.1±0.1 fringes (n), whereas for R-II and R-III the number of fringes obtained were 2.1±0.1, 4.3±0.1, 6.3±0.1; and 2.0±0.1, 4.3±0.1, and 6.2±0.1, respectively, as shown in Figure S3(a)-S3(c). The corresponding thicknesses of the ices were calculated using equation 2 (Table 3).      The spectra revealed significant absorptions in the 500 cm-1 to 1500 cm-1 range due to fundamental bands along with a number of combination bands and overtones. To accurately assign fundamental bands at 10 K, we employed electronic structure theory calculations of the molecules and summarized in Table 4a – 6a. The combination and overtone modes of each refrigerant are summarized in Table 4b – 6b. New vibrational bands (asterisked) emerge for thicker ices as revealed via spectral deconvolution (Figures 3 - 5); (Table S1(a) – S1(c)). The reliability of the computational method is benchmarked by comparing the calculated frequencies with the experimental ones as shown in Figure S1(a)-S1(c); calibration factors are calculated to be 0.983±0.001, 1.004±0.001, and 0.981±0.001 for R-I, R-II, and R-III respectively. A summary of the previously reported spectral bands in the gas, liquid, and solid phases is also provided for comparison of the solid phase spectral frequency with literature assignments. The coordinates of the optimized structures of the refrigerants provided in Tables S2(a) – S2(c), while calculated fundamental frequencies are compiled in Tables 4(a) – 6(a).

The most prominent vibrational features are observed between 1000 cm-1 and 1400 cm-1, mainly involving C—F vibrations. As there exists a significant number of vibrational modes, we are limiting our discussion to the five most intense fundamental vibrational modes for spectral shifts and intensity changes with respect to the vapor phase spectra as well as with ice layer thicknesses for each of the refrigerants. The fundamental and the combination/overtone modes of the refrigerants used in this study are represented in terms of νn (R-I/R-II/R-III) and Cn (R-I/R-II/R-III), respectively, where n is an integer number. As an example, first fundamental and combination modes of R-I is denoted as ν1 (R-I) and C1 (R-I) respectively. The combination frequencies are marked from higher to lower frequency to avoid more complications (Tables 4(b) – 6(b)) and the fundamental modes are assigned according to previous studies are mentioned in Tables 4(a) – 6(a).

Figure 3: Infrared spectra of 1,1,1,2-tetrafluoroethane (R-I) at different ice thicknesses of (a) 518±16 nm; (b) 1037±21 nm, and (c) 1556±24 nm.

Table 4a: Band strengths for the modes of 1,1,1,2-tetrafluoroethane (CF3CH2F) (R-I)

| Fundamental modes assigneda | Experimental frequency 10 Ka (cm-1) | Calculated frequencya (cm-1) | Band strength (10-18 cm molecule-1) | Solid phase infrared frequency at 150 K34 (cm-1) | Raman peak of liquid at 203 K33,34 (cm-1) | Gas phase infrared frequency at 298 Ka,35,36 (cm-1) | Assignmenta,36 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ν12 | 3045 | 3125 | 0.08±0.01 |  | 3030 | 3013 | σas (CH2); |
| ν1 | 3002 | 3065 | 0.53±0.06 |  | 2990 | 2986 | σs (CH2); |
| ν2 | 1462 | 1495 | 0.73±0.06 |  |  | 1464 | β (CH2) scissoring; |
| ν3 | 1429 | 1441 | 1.08±0.08 | 1427 |  | 1427, 1419 | ω(CH2) / σ (CC); |
| ν13 | 1301-1292 | 1306 | 2.63±0.49 |  |  | 1301 | β (CC) / τ (CH2 out of plane); |
| ν4 | 1283-1277 | 1289 | 1.20±0.17 | 1279 | 1284 | 1299, 1292 | ω(CH2) + δs(CF3) + σ (CC); |
| ν14 | 1192-1181 | 1194 | 3.18±0.28 |  |  | 1203 | νas (CF) + τ (CH2 in plane); |
| ν5 | 1166-1161 | 1160 | 1.76±0.08 | 1167 | 1173 | 1189, 1182 | σ s (CF) + ω(CH2); |
| ν6 | 1081, 1060 | 1103 | 1.06±0.07 | 1069 | 1061 | 1070 | σ (CF of CH2F) / σ (CC); |
| ν15 | 971 | 976 | 0.75±0.23 | 965 | 968 | 972 | ρ(CH2) + b (CF of CH2F); |
| ν7 | 841 |  | 0.49±0.04 | 839 | 837 | 844, 847 | σs(CF3) / σ (CC); |
| ν8 | 664 | 664 | 0.72±0.09 | 660 | 660 | 666, 658 | δs(CF3) /δ(CH2F); |
| ν9 | 550 | 550 | 0.20±0.02 | 550 | 548 | 557 | δs (CF3); |
| ν16 | 533 | 535 | 0.07±0.01 | 534 |  | 542 | δas (CF3); |
| ν10 |  | 418 |  | 411 | 407 | 410 | δas (CF3) /δ(CH2F); |
| ν17 |  | 374 |  | 357 | 358 | 362, 354 | ρ(CF3) / ρ(CH2); |
| ν11 |  | 240 |  |  |  | 222 | ρ(CF3) / ρ(CH2F); |
| ν18 |  | 166 |  | 124 |  | 112 | Torsion; |

ν: Frequency; σ: Stretching; β: Bending; ρ: Rocking; δ: Deformation; ω: Wagging; τ: Twisting; a: This study

Table 4b: Band strengths for the modes of 1,1,1,2-tetrafluoroethane (CF3CH2F) (R-I)

| Combination modes assigneda | Experimental frequency 10 Ka (cm-1) | Band strength (10-19 cm molecule-1) | Solid phase infrared frequency 150 K | Raman liquid 203 K34 | Gas phase infrared frequency 298Kb | Assignmenta |
| --- | --- | --- | --- | --- | --- | --- |
| C1 | 4475 | 1.50±0.14 |  |  |  | ν12 + ν2 |
| C2 | 4436 | 0.24±0.04 |  |  |  | ν1 + ν2 |
| C3 | 2910 | 0.62±0.06 |  |  | 2912 | 2ν2 |
| C4 | 2885 | 0.24±0.02 |  |  | 2887 | ν2 + ν3 |
| C5 | 2586 | 0.32± 0.01 |  |  |  | ν13 + ν4 |
| C6 | 2469 | 0.74±0.02 |  |  |  | ν4 + ν14 |
| C7 | 2417 | 0.32±0.07 |  |  | 2424 | ν2 + ν15 |
| C8 | 2396 | 0.29±0.01 |  |  |  | ν13 + ν15 |
| C9 | 2354 | 0.63±0.07 |  |  | 2359 | ν4 + ν6 |
| C10 | 2267 | 0.48±0.07 |  |  | 2267 | ν4 + ν15 |
| C11 | 2253 | 0.88±0.02 |  |  |  | ν5 + ν15 |
| C12 | 2129 | 1.71±0.05 |  |  | 2137 | 2ν6 |
| C13 | 2010 | 0.42±0.01 |  |  |  | ν2 + ν9 |
| C14 | 1930 | 0.35±0.01 |  |  | 1945 | 2ν15 |
| C15 | 1832 | 0.91±0.10 |  |  | 1831 | ν3 + ν10 |
| C16 | 1390 | 1.65±0.15 | 1386 | 1389 | 1382 | ν7 + ν16 |
| C17 | 1374 | 2.09±0.19 | 1372 |  | 1374 | ν10 + ν15 |
| C18 | 1249 | 1.05±0.03 |  |  |  | ν15 + ν17 |
| C19 | 1210 | 11.82±1.51 |  |  |  | ν8 + ν16 |
| C20 | 820 | 0.39±0.01 | 820 |  |  | 2ν10 |
| C21 | 687 | 1.09±0.03 |  |  | 673 | ν10 + ν11 |

Figure 4: Infrared spectra of 2,3,3,3-tetrafluoropropene (R-II) at different ice thicknesses of (a) 504±15 nm; (b) 1015±18 nm, and (c) 1486±21 nm.

Table 5a: Fundamental modes of 2,3,3,3-tetrafluoropropene (CF3CF=CH2) (R-II)

| Fundamental modes assigneda | Experimental frequency 10 Ka (cm-1) | Calculated frequencya (cm-1) | Band strength (10-18 cm molecule-1) | Solid phase Raman frequency 150 K37,38 | Raman liquid 203 K37,38 | Gas phase infrared frequency 298 Ka,37,38 | Assignmenta,37 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ν1 | 3159 | 3280 | 0.48±0.06 | 3160 | 3158 | 3161 | σas (CH2); |
| ν2 | 3052 | 3181 | 0.29±0.04 | 3037 | 3036 | 3055 | σs (CH2); |
| ν3 | 1700 | 1751 | 1.27±0.08 | 1700 | 1698 | 1700 | σ (C=C); |
| ν4 | 1395 | 1359 | 1.17±0.41 | 1390 | 1388 | 1391 | ρ(CH2) / σas (CF3); |
| ν5 | 1365, 1350 (PR) |  | 0.83±0.07 | 1347 | 1352 | 1357 | σ (C—F of alkene) / β (C—C); |
| ν6 | 1200-1205 | 1184 | 0.68±0.05 | 1192 | 1208 | 1210 | σas (CF3) / β (CH2) scissoring/ β (C—F of alkene); |
| ν15 | 1173-1166 | 1155 | 2.74±0.29 | 1161 | 1162 | 1181 | δs (CF3)/ σ (C—F of alkene)/ ρ(CH2); |
| ν7 | 1137-1162 | 1148 | 0.87±0.07 | 1134 |  | 1162 | σs (CF3)/ τ (CH2); |
| ν8 | 939 | 961 | 0.68±0.04 | 938 | 942 | 945 | ρ(CH2)/ σ (C—F of alkene); |
| ν16 | 914-901 | 929 | 0.99±0.18 | 910 | 902 | 889 | ω(CH2)/ β (C=C); |
| ν9 | 789 | 786 | 0.11±0.01 | 790 | 790 | 793 | σ (C—C)/ ρ(CH2)/ δs(CF3); |
| ν10 | 615 | 611 | 0.22±0.04 | 614 | 616 | 615 | δ (CCF) in plane/ ρ(CH2); |
| ν11 | 575 | 571 | 0.13±0.01 | 576 | 576 | 579 | δs(CF3)/ ρ(CH2); |
| ν19 |  | 493 |  | 497 | 497 |  | δas (CF3)/ τ (CH2)/ δ (CCF) out of plane; |
| ν12 |  | 415 |  | 423 | 421 |  | δ (CCC) in plane; |
| ν13 |  | 370 |  | 370 | 367 |  | δ(C=C—F) in plane; |
| ν20 |  | 240 |  | 237 | 239 |  | δ (CF3); |

Table 5b: Combination modes of 2,3,3,3-tetrafluoropropene (CF3CF=CH2) (R-II)

| Combination modes assigneda | Experimental frequency 10 Ka (cm-1) | Band strength (10-19 cm molecule-1) | Solid phase Raman frequency 150 K38 | Gas phase infrared frequency 298 Ka,37 | Assignmenta |
| --- | --- | --- | --- | --- | --- |
| C1 | 4497 | 0.58±0.04 |  | 4503 | ν1 + ν5 |
| C2 | 4292 | 0.23±0.05 |  | 4305 | ν1 + ν6 |
| C3 | 4091 | 0.46±0.05 |  | 4100 | ν1 + ν8 |
| C4 | 3387 | 0.64±0.06 |  | 3393 | 2ν3 |
| C5 | 3093 | 0.68±0.10 | 3094 | 3096 | ν3 + ν4 |
| C6 | 3062 | 1.81±0.31 | 3062 | 3070 | ν3 + ν9 + ν11 |
| C7 | 2740 | 0.15±0.04 |  | 2749 | ν4 + ν5 |
| C8 | 2700 | 0.09±0.01 |  | 2708 | 2ν5 |
| C9 | 2631 | 0.48±0.10 |  | 2644 | ν3 + ν8 |
| C10 | 2596 | 0.23±0.03 |  |  | ν4 + ν6 |
| C11 | 2555 | 0.17±0.02 |  |  | ν4 + ν15 |
| C12 | 2485 | 0.05±0.01 |  |  | ν3 + ν9 |
| C13 | 2195 | 0.14±0.02 |  | 2202 | ν4 + ν9 |
| C14 | 2177 | 0.19±0.05 |  | 2180 | ν5 + ν9 |
| C15 | 2139 | 0.23±0.01 |  | 2146 | ν5 + ν9 |
| C16 | 2077 | 0.24±0.05 |  | 2099 | ν5 + ν8 |
| C17 | 1982 | 0.31±0.02 |  | 1996 | ν3 + ν10 |
| C18 | 1936 | 0.55±0.10 |  | 1943 | ν15 + ν7 |
| C19 | 1876 | 0.87±0.12 |  | 1893 | 2ν11 + ν9 |
| C20 | 1815 | 0.95±0.11 |  | 1823 | 2ν8 |
| C21 | 1406 | 13.01±0.08 | 1408 |  | β (CH2) scissoring + (C—C) bending |
| C22 | 1334 | 0.78±0.10 |  | 1356 | ν8 + ν16 |
| C23 | 1285 | 0.76±0.04 |  | 1291 | ν9 + ν11 |
| C24 | 1224 | 12.45±1.51 |  |  | ν12 + ν16 |
| C25 | 1133-1125 | 2.24±0.10 |  | 1114 | 2ν11 |
| C26 | 1086 | 1.45±0.15 |  | 1088 | ν11 + ν19 |

Figure 5: Infrared spectra of 3,3,3-Trifluoropropene (R-III) at different ice thicknesses (a) 486±14nm; (b) 1046±20 nm, and (c) 1508±26 nm.

Table 6a: Fundamental modes of 3,3,3-trifluoropropene (CF3CH=CH2) (R-III)

| Fundamental mode assigneda | Experimental frequency 10 Ka (cm-1) | Calculated frequencya (cm-1) | Band strength (10 -18 cm molecule-1) | Solid phase infrared frequency 150 K39 | Raman liquid 203 K39 | Gas phase infrared frequency 298 Ka,40,41 | Assignmenta,40,41 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ν1 | 3125, 3110 | 3244 | 0.06±0.01 | 3113 | 3127 | 3124 | σas (CH2); |
| ν2 | 3070 | 3188 | 0.06±0.01 | 3073 | 3066 | 3066 | σ (CH adjacent to CF3); |
| ν3 | 3022 | 3155 | 0.04±0.01 | 3021 | 3021 | 3016 | σs (CH2); |
| ν4 | 1662 | 1723 | 0.28±0.02 | 1673 | 1662 | 1671 | σ (C=C); |
| ν5 | 1432 | 1461 | 0.47±0.09 | 1429 | 1432 | 1433 | β (CH2) scissoring/ β (C=CH)/ β (C—C); |
| ν6 | 1311 | 1329 | 0.99±0.15 | 1313 | 1312 | 1311 | ρ(HC=CH)/ δs (CF3); |
| ν7 | 1276-1280 | 1282 | 0.86±0.17 | 1285 | 1284 | 1285 | σas (CF3)/ ρ(HC=CH)/ β(C—C); |
| ν8 | 1152-1168 | 1164 | 2.41±0.26 | 1183 | 1169 | 1182 | σas (CF3)/ ρ (HCH)/ δ (C=C—C) in plane; |
| ν15 | 1119-1133 | 1125 | 2.35±0.35 | 1156 | 1143 | 1160 | σas (CF3)/ τ (HCH) in plane/ δ (C=C—C) out of plane |
| ν9 | 1016 | 1031 | 0.80±0.20 | 1009 | 1017 | 1021 | ρ (CH2)/ δ (C=C—C) in plane; |
| ν16 | 984 | 1016 | 0.79±0.08 | 980 | 968 | 980 | τ (HCH) out of plane/ τ (HC=CH) out of plane; |
| ν17 | 974 | 1002 | 0.93±0.14 | 963 | 960 | 889 | ω(CH2)/ δ (HC=C) out of plane; |
| ν10 | 806 | 806 | 0.03±0.01 | 805 | 808 | 810 | σs (CF3)/ β (HC=C) in plane/ ρ(CH2); |
| ν18 | 706 | 719 | 0.09±0.01 | 700 | 708 | 705 | σs (CF3)/ β (HC=C) out of plane/ ρ(CH2) [ν18] |
| ν11 | 634 | 611 | 0.08±0.01 | 614 | 616 | 615 | δ (CCF) in plane/ ρ(CH2); |
| ν12 | 554 | 541 | 0.09±0.01 | 556 | 547 | 553 | δas (CF3)/ τ (HCH) out of plane/ σ (C—C)/ δ (C=C—C) in plane; |
| ν19 | 546 | 511 | 0.09±0.01 | 544 | 521 | 543 | δas (CF3)/ δ(C=C—C) out of plane; |
| ν13 |  | 429 |  | 423 | 432 | 431 | β (C=C—C) in plane/ ρ (CF3); |
| ν20 |  | 314 |  | 320 | 312 | 317 | β (C=C—C) out of plane + ρ (CF3); |
| ν14 |  | 279 |  | 237 | 239 |  | ρ (CF3); |

Table 6b: Combination modes of 3,3,3-trifluoropropene (CF3CF=CH2) (R-III)

| Combination modes assigneda | Experimental frequency 10 Ka (cm-1) | Band strength (10 -19 cm molecule-1) | Assignmenta |
| --- | --- | --- | --- |
| C1 | 4541 | 0.70±0.06 | ν1 + ν5 |
| C2 | 4489 | 0.14±0.03 | ν1 + ν6 |
| C3 | 4133 | 0.14±0.01 | ν1 + ν15 |
| C4 | 2944 | 0.39±0.08 | ν4 + ν6 |
| C5 | 2714 | 0.38±0.06 | ν4 + ν15 |
| C6 | 2669 | 0.11±0.05 | ν5 + ν7 |
| C7 | 2560 | 0.26±0.02 | ν5 + ν15 |
| C8 | 2282 | 1.05±0.17 | ν7 + ν9 |
| C9 | 2237 | 0.61±0.15 | ν8 + ν15 |
| C10 | 2116 | 0.17±0.03 | ν9 + ν16 |
| C11 | 2087 | 0.30±0.01 | ν7 + ν10 |
| C12 | 2031 | 0.21±0.03 | ν15 + ν17 |
| C13 | 1952 | 2.60±0.18 | ν16 + ν17 |
| C14 | 1919 | 0.35±0.02 | 2ν17 |
| C15 | 1675 | 1.25±0.18 | ν16 + ν11 |
| C16 | 1411 | 2.43±0.35 | ν13 + ν17 |
| C17 | 1352 | 1.36±0.05 | ν10 + ν20 |
| C18 | 1294 | 27.83±1.91 | ν11 + ν19 |
| C19 | 1181 | 11.73±1.03 | ν10 + ν12 |
| C20 | 1114 | 7.39±0.64 | 2ν12 |
| C21 | 1034 | 1.26±0.40 | ν11 + ν13 |

3.2.1.1 Spectral Shifts and Intensity Alteration in Ices Compared to the Gas Phase

Vapor-deposited, low-temperature solid phase infrared spectra of all the refrigerants used in this study induces significant change in spectral intensity pattern and spectral shift in major fundamental vibrational modes with respect to their vapor phase infrared spectra, as well as with the variation of the thickness of ice. Most of the HFCs has significant absorption in the 500 cm-1 to 2000 cm-1 region corresponding to the most prominent fundamental modes. Infrared spectral changes at different thickness of ices with vapor phase infrared spectra for each of the refrigerant in this region is compared in Figure 6(a) - 6(c) and full infrared vapor phase spectra is provided in Figure S4(a)-S4(c).

The C—F vibrational modes associated with the CF3 group reveal the strongest absorptions among all vibrational modes irrespective of the nature of the refrigerant. Apart from these C—F stretching modes, R-I and R-II carry F atom bonded to sp3 and sp2 hybridized carbon atoms. In all cases, the C—F stretching modes are coupled with, e.g., CH2 bending, C—C stretching, and C—C bending modes. Significantly, the CH2 bending modes like scissoring, wagging – coupled with C—C stretching and C—C bending – do not exhibit any spectral shifts when between the gas phase spectra and ices. As an example in case of (R-I), the vibrational modes associated with CH2 scissoring contributed with C—C bending (ν2 (R-I): 1462 cm-1) and CH2 wagging (ω) contributed with C—C stretching (ν3 (R-I): 1429 cm-1) does not exhibit spectral shifts. However, there is an increase in relative intensity of these modes in the solid phase compared to the gas phase indicating amorphous morphology in solid phase affecting modes with respect to gas phase which needs further theoretical calculation to get further insights. A similar trend is also observed in the case of olefinic HFCs (HFO), but apart from the CH2 bending modes, C—C vibrational modes associated with the C=C moiety are also observed. In all cases, the C=C stretching modes do not show spectral shifts with respect to the gas phase spectra or distinct ice thicknesses. However, the individual spectral position of the C=C stretching modes are distinct. The C=C stretching mode for 2,3,3,3-tetrafluoro propene (R-1234yf), where a fluorine atom is bonded to the olefine, is at higher frequency (ν3(R-II): 1701 cm-1) compared to same C=C (ν5 (R-III): 1662 cm-1) for 3,3,3-trifluoropropene (R-III), where no fluorine atom is bonded to the olefinic moiety.  Besides the increase in the stretching frequency, a similar trend is noticeable for the relative intensities of the C=C modes which indicates bonding with a fluorine atom to the carbon-carbon double bond induces larger changes in the dipole moment. The following section describes distinct C—F vibrational modes coupled with associated modes in terms of vibrational shifts, intensities, and spectral broadening for the refrigerants used in this study.

Apart from the existence of vibrational shifts of refrigerant ice at 10 K with respect to gas phase spectra, change in spectral pattern corresponding to C—F vibrational modes within the region 2000 cm-1 to 500 cm-1 also has been observed at 80 K for non-olefinic refrigerant 1,1,1,2-tetrafluoroethane and at 70 K for rest of the olefinic refrigerants (2,3,3,3-tetrafluoropropene & 3,3,3-trifluoropropene), indicating formation of crystalline phase.[54],[55] As the primary objective of this study is to quantify optical spectroscopic parameter and understanding vibrational shifts, variation in spectral pattern due to phase shift are provided in supporting information S5(a)-S5(c) as a general observation during sublimation of refrigerant ices. However, further combined experimental and theoretical study in this direction could stipulate further insights towards the phase transition of the refrigerants used in this study.

1,1,1,2-tetrafluoroethane (CF3CH2F) (R-I)

The most intense C—F vibrational modes along with C—H and C—C modes likely remain in the 1328 cm-1 to 1260 cm-1 and 1238 cm-1 to 1154 cm-1 regions; the first region corresponds to fundamental modes of CH2 wagging (ω) having contributions from the C—C stretching (σ) and CF3 deformation (δCF3), while the second region corresponds to CF3 stretching (σCF3) fundamentals with contributions from C—H and C—C bending modes (Figure 6a). These fundamental modes where contribution from C—F vibrational mode exists, induces frequency redshift in the solid ices as compared to vapor phase due to intermolecular interactions through in F···H.  For example, fundamental CF3 stretching mode in the ices (ν5 (R-I)) undergoes a red-shift from 1184 cm-1 in the gas phase to 1161 cm-1 for the 1556±24 nm thick ice. The concerned mode has a contribution from CH2 wagging (ω). On the other hand, the fundamental CH2 wagging (ω) (ν4 (R-I)) is also red-shifted from 1292 cm-1 in the gas phase to 1283 cm-1 in the ice of 518±16 nm thickness, which is further red-shifted towards 1277 cm-1 for a thicker ice of 1556±24 nm due to significant contribution of CF3 deformation (δCF3) mode, which usually undergoes spectral redshift as mentioned earlier. Apart from the modes associated with the contribution from C—F vibrations arising from CF3, C—F vibration arising from adjacent CH2F moiety also induces frequency red shifting in the solid ices as compared to vapor phase.

Figure 6: Comparison of infrared spectra of the refrigerants in the vapor phase and solid phase experimentally measured in this study. (a) 1,1,1,2-tetrafluoroethane R-I at ice thicknesses of 518±16 nm, 1037±21 nm, 1556±24 nm; (b) 2,3,3,3-tetrafluoropropene R-II at ice thicknesses of 504±15 nm, 1015±18 nm, 1486±21 nm; (c) 3,3,3-trifluoropropene R-III at thicknesses of 486±14 nm, 1046±20 nm, 1508±26 nm.

Although the extent of red shift is more dominant involving this C—F vibration (30 cm-1) compared to the other originated from CF3 (15 cm-1 to 20 cm-1). The extent of red shift remains same with the increase of ice thickness which indicates this C—F stretching is not affected with layer of ice formation. The other low frequency modes in the ices below 1000 cm-1 region do not show any significant red-shifts with respect to the gas phase spectra.

2,3,3,3-tetrafluoropropene (CF3CF=CH2) (R-II)

This new-generation HFO is a quite distinct as R-II carries a fluorine atom at the olefinic (C=C) moiety. The presence of this fluorine induces significant coupling with the C=C group leading to closely associated vibrational modes even in gas phase unlike R-I (Figure 6b). Most of the fundamental CH2 bending modes like rocking (ρ) and twisting (τ) not only have contribution from the C—F stretching and bending modes originating from CF3, but also from the C—F moiety of the sp2 hybridized carbon atom. Although the modes are closely associated, the vibrational mode ν15 (R-II) consisting C—F stretching of olefinic-bounded CF along with other modes CH2 scissoring and C—F deformation (δCF3) of CF3, exhibits same extent of red-shifting in different thickness of solid ices (1170 cm-1) compared to the gas phase spectra (1181 cm-1) like to the case of R-I. On the other hand, increase in red shift with the extent of ice thickness compared to gas phase in the case of ν6 (R-II) and ν7 (R-II) fundamental mode, carrying symmetric and asymmetric C—F stretching of CF3 group indicates involvement of C—F stretching of CF3 in ice layer formation via intermolecular H-bonding interactions, weakening the C-F bond.

In addition to the modes similar to R-I, this olefinic refrigerant has C=C—F vibrations (stretching or bending) which exhibit two distinct modes with respect to the molecular plane: in plane and out of plane. Distinct spectral shifts are observed within two fundamental modes ν8 (R-II) & ν16 (R-II) in the ices as compared to the gas phase spectra. The first mode, where the fundamental CH2 rocking (ρ) mode has contribution from the in-plane C=C—F vibration, experiences a red shift from 949 cm-1 to 939 cm-1, while the second mode exhibits an unusual blue shift from 890 cm-1 to 910 cm-1; here, along with the CH2 wagging (ω) fundamental mode contribution from out of plane C=C—F vibrational mode exists. However, both modes are not further red or blue shifted with increasing thicknesses of the ice layers. This unusual blue shift of CH2 wagging (ω) fundamental mode possibly occurred due to repulsive interaction.[56, 57]

3,3,3-trifluoropropene (CF3CH=CH2) (R-III)

This simple HFO shows similar thermodynamic property with R-II, but when structurally compared with R-II, this refrigerant does not carry any olefinic bounded fluorine atom. The C—F vibrations for R-III originates from CF3 group only. The absence of the olefine bonded fluorine atom induces less coupling between the vibrational modes, which is evident from the experimentally measured vapor phase vibrational spectra of R-II and R-III. Most of the CF3 fundamental vibrational modes remain mixed with olefinic modes like HC=CH bending and C=C—C bending (Figure 6c and Table 6a). All C—F stretching fundamental modes experience redshifts in the solid phase spectra. The HC=CH bending mode coupled with C—F stretching fundamental mode (ν7 (R-III)) reveal redshifts (1280 cm-1 – 1276 cm-1) compared to gas phase (1285 cm-1) as evident from Figure 6c. The olefinic C=C—C moiety has two type of modes as in-plane and out-of-plane which contribute to the fundamental CF3 stretching and generate two types of CF3 stretching ν8 (R-III) and ν15 (R-III), respectively. These modes are redshifted in solid ices as compared to vapor phase like all other cases. Apart from the C=C—C vibration, the C=C—H moiety results in similar vibrations like the C=C—F moiety in R-II. The out-of-plane C=C—H contributed fundamental mode of CH2 wagging (ω) (ν17 (R-III) exhibits blue shifts, as in the case of R-II, due to the formation of a less mobile, regular lattice structure. However, the extent of these blue shifts is lower compared to R-II due to the absence of directly bound F induces less steric repulsion.

3.2.2 Infrared Band Strength Measurements

The infrared spectroscopic data are key for the quantification of upper tropospheric species either in the form of gas, liquid, or solid. Infrared intensities of low-temperature ices are quantified in terms of band strengths (in cm molecule-1). Experimentally measured integrated absorbances (Adν ) are utilized to evaluate the band strengths as they are related through equation 6[58, 59] where ρ = mass density; NA = Avogadro number; M = molar mass; L = optical path length and A′= band strength.

Adν=ρNAA'2.303ML                                                               (6)

In our measurements, densities of R-I, R-II, and R-III are taken from crystallographic data at low temperatures. Both R-I and R-II forms body centered cubic (bcc) lattice with density 1.77 g cm-3 and 1.74 g cm-3 respectively.[38, 60] Both R-I and R-II contain a CF3 group. In case of R-III, low-temperature crystallographic data are not available best to our knowledge and since it also contains CF3 group the density of R-III is considered as average density of functionally similar R-I and R-II.

Unlike the gas phase infrared spectra, spectra of solid ices are broad with widths exceeding 4 cm-1. Experimentally measured spectra were analyzed through deconvolution. The integrated areas of the deconvoluted peaks were plotted versus the optical path length (L) to determine band strengths from the slope as described in equation 6. The plots of the integrated area versus optical path length (L) are nearly linear. A plot of integrated area with respect to path length (L) for R-I is provided as a representative in Figure S6. The band strengths of the fundamental bands determined through the analysis are provided in Table 4(a) - 6(a). Similarly, Table 4(b) - 6(b) provides band strengths for the infrared analysis of combination bands. From the analysis of the band strengths, it is quite evident that the most intense frequency among all the frequencies for all refrigerants is C—F vibrational (bending or stretching) modes originating from CF3. In case R-I CF3 deformation contributed CH2 twisting mode ν14 (R-I) within 1180-1191 cm-1 is the strongest having band strength (A′) of 3.18±0.28 × 10-18 cm molecule-1. However, in case of R-II, due to enhanced coupling with F atom directly bound to C=C moiety, the highest intensity vibrational mode corresponds to C—F stretching mode originating from olefine bound F. Thus, ν15 (R-II) is the strongest one having band strength of 2.74±0.29 × 10-18 cm molecule-1. Another olefin which does not contain directly bound F with olefine has the highest band strength for the vibrational mode ν8 (R-III) where asymmetric CF3 stretch is coupled with CH2 and C=C—C bending.

Conclusion

Refrigerant recycling, purification, and low-temperature molecular interactions of refrigerants in the upper troposphere represent fundamental physico-chemical processes. Laboratory experiments require key optical and spectroscopic parameters, such as refractive indices and band strengths, which are often absent at low temperatures. Here, experimentally measured refractive indices of important refrigerants 1,1,1,2-tetrafluoroethane (CF3CH2F; HFC134a), 2,3,3,3–tetrafluoropropene (CF3CF=CH2; R1234yf), and 3,3,3–trifluoropropene (CF3CH=CH2; R1243zf) were evaluated to be 1.24 ± 0.02, 1.34 ± 0.02, and 1.30 ± 0.02, respectively.  Further, the analysis of vibrational assignments of HFCs was well supported by electronic structure calculations. The reliability of the computational method is benchmarked by comparing the calculated frequencies with those obtained experimentally. Calibration factors are calculated to be 0.983±0.001, 1.004±0.001, and 0.981±0.001 for CF3CH2F, CF3CF=CH2, and CF3CH=CH2, respectively. All HFCs carry a CF3 group which typically contributes the most intense vibrational mode, with band strengths in the range of 2×10-18 to 3×10-18 cm molecule-1. However, in the olefine 2,3,3,3-tetrafluoropropene (R-1234yf) (R-II), the strongest vibration originates from olefine bound C—F bond. The optical parameter refractive index (ƞR) and band strength (A′) are interrelated, as optical pathlength (L) which used in the determination of band strength (A′) is related dependent on refractive index (ƞR) through equations 2,3 and 4. A comparison of the solid-state spectra with the gas-phase infrared spectra reveals that most of the C—F stretching frequencies are redshifted. Overall, through our quantitative investigation of key optical and spectroscopic parameters, an unexplored yet essential inventory to understand low-temperature data of HFCs were collected and presented. Apart from that amorphous to crystalline phased transformations are also evidenced exploiting absorption reflection absorption infrared spectroscopy, further theoretical calculation could provide further insights towards evidenced phase transitions.

Supporting information available:

Calibration of calculated frequency with experimental ones (Figure S1); Experimentally measured interference patterns for methane (Figure S2); Interference patterns of different refrigerants observed during deposition (Figure S3); Combination bands arise at higher thicknesses of refrigerant ices (Table S1); Optimized coordinates of the refrigerants (Table S2); Experimentally measured vapor phase infrared spectra of the refrigerants (Figure S4); Evidence of crystalline phase transformation at elevated temperature (Figure S5); Representative plot of integrated areas versus ice thicknesses utilized to measure band strengths (Figure S6).

Competing interests: The authors declare no competing interest.

Data Availability:

All the data are included in the manuscript and/or supporting information.

Competing interests: The authors declare no competing interest.

Data Availability:

All the data are included in the manuscript and/or supporting information.

Acknowledgements:

This study was funded through the NSF award, 2330175, Center: NSF Engineering Research Center for Environmentally Applied Refrigerant Technology Hub.

References:

[1]	F. Pardo, G. Zarca, A. Urtiaga, ACS Sustain. Chem. Eng. 2020, 8, 2548-2556.

[2]	P. Dewapriya, L. Chadwick, S. G. Gorji, B. Schulze, S. Valsecchi, S. Samanipour, K. V. Thomas, S. L. Kaserzon, J. Hazard. Mater. Lett. 2023, 4, 100086.

[3]	D. W. Phelps, L. V. Parkinson, J. M. Boucher, J. Muncke, B. Geueke, Environ. Sci. Technol. 2024, 58, 5670-5684.

[4]	S. Hamlin, R. Hunt, S. Tassou, Appl. Therm. Eng. 1998, 18, 1139-1148.

[5]	X. Liu, T. Zhang, Q. Gao, X. Xu, H. Chen, S. Wang, Appl. Therm. Eng. 2024, 236, 121613.

[6]	Z. Zhou, B. Chen, Y. Wang, L. Guo, G. Wang, Appl. Therm. Eng. 2012, 39, 29-36.

[7]	K. N. Taddonio, G. B. Dreyfus, S. O. Andersen, A. Ravishankara, Environ. Sci. Technol. 2023, 57, 11731-11737.

[8]	T. Tan, L. Rennels, B. Parthum, Nat Clim Chang 2024, 14, 55-60.

[9]	B. K. Sovacool, S. Griffiths, J. Kim, M. Bazilian, Renew. Sustain. Energy Rev. 2021, 141.

[10]	A. K. Vuppaladadiyam, E. Antunes, S. S. V. Vuppaladadiyam, Z. T. Baig, A. Subiantoro, G. Lei, S.-Y. Leu, A. K. Sarmah, H. Duan, Sci. Total Environ. 2022, 823, 153670.

[11]	T. Tan, L. Rennels, B. Parthum, Nat. Clim. Change 2024, 14, 55-60.

[12]	F. Graziosi, J. Arduini, F. Furlani, U. Giostra, P. Cristofanelli, X. Fang, O. Hermanssen, C. Lunder, G. Maenhout, S. O'Doherty, Atmos. Environ. 2017, 158, 85-97.

[13]	S. Xiaopu, W. Pu, L. Hui, G. Bai-He, W. Yi, Adv. Clim. Change Res. 2022, 13, 564-577.

[14]	X. Ruan, Y. Dai, L. Du, X. Yan, G. He, B. Li, Sep. Purif. Technol. 2015, 156, 673-682.

[15]	H. B. et. al., Perfluorocompound separation and purification method and system. . US- 5779863-A, 1998-07-14, 1998.

[16]	M. W. T. et. al., Reclamation and separation of perfluorocarbons using condensation. US-6383257-B1, 2002-05-07, 2002.

[17]	Drout, W. M. Extractive distillation process. US-2610141-A, 1952-09-09,1952.

[18]	Z. Lei, C. Li, B. Chen, Sep. Purif. Rev. 2003, 32, 121-213.

[19]	E. A. Finberg, M. B. Shiflett, Ind. Eng. Chem. Res. 2021, 60, 16054-16067.

[20]	A. Mota-Babiloni, M. M. Joybari, J. Navarro-Esbrí, C. Mateu-Royo, Á. Barragán-Cervera, M. Amat-Albuixech, F. Molés, Int. J. Refrig. 2020, 111, 147-158.

[21]	Í. F. Guilherme, D. F. M. Pico, D. D. O. dos Santos, E. P. Bandarra Filho, J. Build. Eng. 2022, 47, 103847.

[22]	L. Wang, P. Jiao, C. Dang, E. Hihara, B. Dai, Int. J. Therm. Sci. 2021, 170, 107090.

[23]	V. Nair, Int. J. Refrig. 2021, 122, 156-170.

[24]	X. Zhang, Y. Li, Energy 2024, 311, 133423.

[25]	G. Salierno, Chem. Sus. Chem 2024, 17, e202400280.

[26]	R. Holland, M. A. H. Khan, I. Driscoll, R. Chhantyal-Pun, R. G. Derwent, C. A. Taatjes, A. J. Orr-Ewing, C. J. Percival, D. E. Shallcross, ACS Earth Space Chem. 2021, 5, 849-857.

[27]	J. B. Burkholder, R. Cox, A. Ravishankara, Chem. Rev. 2015, 115, 3704-3759.

[28]	S. Biswas, D. Paul, K. Mondal, R. I. Kaiser, Proc. Natl. Acad. Sci. U.S.A. 2025, 122, e2425543122.

[29]	K. Mondal, S. Biswas, N. Melbourne, R. Sun, R. I. Kaiser, Chem. Sci. 2025, 16, 11039-11048.

[30]	G. E. Morales-Espejel, R. Meeuwenoord, A. F. Quiñonez, R. Hauleitner, Proc. Inst. Mech. Eng. Part C J. Mech. Eng. Sci. 2015, 229, 244-253.

[31]	R. Morse, T. Moreira, J. Chan, K. Dressler, G. Ribatski, E. Hurlburt, L. McCarroll, G. Nellis, A. Berson, Int. J. Heat Mass Transf. 2021, 177, 121487.

[32]	S. Kong, Z. Wang, X. Xu, H. Sun, Z. Liu, Y. Fang, M. Su, H. Yang, Int. J. Multiph. Flow 2022, 153, 104108.

[33]	J. R. Nielsen, C. Halley, J. Mol. Spectrosc. 1965, 17, 341-347.

[34]	W. F. Edgell, T. R. Riethof, C. Ward, J. Mol. Spectrosc. 1963, 11, 92-107.

[35]	D. Harnish, R. Hirschmann, Appl. Spectrosc. 1970, 24, 28-35.

[36]	L.-H. Xu, A. M. Andrews, R. R. Cavanagh, G. T. Fraser, K. K. Irikura, F. J. Lovas, J.-U. Grabow, W. Stahl, M. K. Crawford, R. J. Smalley, J. Phys. Chem. A 1997, 101, 2288-2297.

[37]	A. P. Charmet, L. Bizzocchi, B. M. Giuliano, P. Caselli, N. C. Craig, S. V. Krasnoshchekov, J. Quant. Spectrosc. Radiat. Transf. 2019, 239, 106656.

[38]	M. Feller, K. Lux, C. Hohenstein, A. Kornath, Z. Naturforsch. B 2014, 69, 379-387.

[39]	D. Christen, V. Hoffmann, P. Klaeboe, Z. Naturforsch. A 1979, 34, 1320-1329.

[40]	G. A. Guirgis, H. Zhen, J. B. Robb II, J. R. Durig, Vib. Spectrosc. 2000, 23, 137-150.

[41]	A. Ainetschian, G. T. Fraser, B. H. Pate, R. Suenram, Chem. Phys. 1995, 190, 231-245.

[42]	A. M. Turner, M. J. Abplanalp, R. I. Kaiser, Astrophys. J. 2016, 819, 97.

[43]	M. McAnally, J. Bocková, A. M. Turner, N. Hara, D. Mikhnova, C. Meinert, R. I. Kaiser, Proc. Natl. Acad. Sci. U.S.A. 2025, 122, e2501839122.

[44]	C. Zhu, A. M. Turner, M. J. Abplanalp, R. I. Kaiser, B. Webb, G. Siuzdak, R. C. Fortenberry, Astrophys. J. Lett. 2020, 899, L3.

[45]	A. M. Turner, M. J. Abplanalp, A. Bergantini, R. Frigge, C. Zhu, B.-J. Sun, C.-T. Hsiao, A. H. Chang, C. Meinert, R. I. Kaiser, Sci. Adv. 2019, 5, eaaw4307.

[46]	A. M. Turner, A. Bergantini, M. J. Abplanalp, C. Zhu, S. Góbi, B.-J. Sun, K.-H. Chao, A. H. Chang, C. Meinert, R. I. Kaiser, Nat. Commun. 2018, 9, 3851.

[47]	A. U. Aldiyarov, D. Y. Sokolov, A. Y. Nurmukan, M. A. Ramos, ACS Omega 2020, 5, 11671-11676.

[48]	M. Domingo Beltrán, R. Luna Molina, M. Á. Satorre Aznar, C. Santonja Moltó, C. Millán Verdú, Sensors 2015, 15, 25123-25138.

[49]	E. Apra, E. J. Bylaska, W. A. De Jong, N. Govind, K. Kowalski, T. P. Straatsma, M. Valiev, H. J. van Dam, Y. Alexeev, J. Anchell, J. Chem. Phys. 2020, 152.

[50]	M. W. Wong, Chem. Phys. Lett. 1996, 256, 391-399.

[51]	A. Siiskonen, A. Priimagi, J. Mol. Model. 2017, 23, 50.

[52]	 (May 2022) ed., National Institute of Standards and Technology.

[53]	M. Bouilloud, N. Fray, Y. Bénilan, H. Cottin, M.-C. Gazeau, A. Jolly, Mon. Not. R. Astron. Soc. 2015, 451, 2145-2160.

[54]	D. Yerezhep, A. Akylbayeva, O. Golikov, D. Y. Sokolov, A. Shinbayeva, A. U. Aldiyarov, ACS Omega 2023, 8, 19567-19574.

[55]	A. Drobyshev, A. Aldiyarov, A. Nurmukan, D. Sokolov, A. Shinbayeva, Low Temperature Physics 2018, 44, 831-839.

[56]	W. Wang, Y. Zhang, B. Ji, J. Phys. Chem. A 2010, 114, 7257-7260.

[57]	X. Li, L. Liu, H. B. Schlegel, J. Am. Chem, Soc. 2002, 124, 9639-9647.

[58]	R. L. Hudson, P. A. Gerakines, Y. Y. Yarnall, Astrophys. J. 2024, 970, 108.

[59]	J. He, S. J. Diamant, S. Wang, H. Yu, W. R. Rocha, M. Rachid, H. Linnartz, Astrophys. J. 2022, 925, 179.

[60]	M. Brunelli, A. Fitch, Zeitschrift für Kristallographie-Crystalline Materials 2002, 217, 395-400.

Table of Contents

Spectroscopic quantification of refrigerants in low temperature for future technological applications and understanding unexplored upper tropospheric chemistry